## Slide 1: MOSFET dosimeter: Definition of MOSFET
MOSFET → acronym for Metal-Oxide Semiconductor Field Effect Transistor
Field effect transistor → use of an electric field to control the shape and the conductivity of a « channel » in a semiconductor material → modulation of the current passing through (between the « source » and the « drain ») with a voltage applied on the central electrode called « gate »
For the MOSFET → the gate (metal or polycrystalline silicon) is electrically isolated from the substrate (semiconductor) by a dielectric (as SiO2) → no current injected by the gate
Can be n- or p-type channel

## Slide 2: Scheme of a n-type channel MOSFET (nMOS)
Typical characteristics → L ≈ 1-40 ¹m, SiO2 thickness ≈ 0.02-0.1 ¹m, ? width ≈ 2-500 ¹m, n regions strongly doped (n+): n ≥ 1017 cm-3

## Slide 3: Principle of operation (n channel)
Assumptions:
  VS = VB
  We apply a positive difference of potential VDS = VD - VS > 0 between the drain and the source
Without grid polarization → VGB = VG - VB = VGS = 0 → no current between the source and the drain → ID = 0
VGS ↗ →
  VGS ≤ VTH → ID = 0 → Cutoff mode: when the gate voltage is smaller than the « threshold voltage »
    → h+ repelled to the substrate → creation of a depletion zone
    → e- thermally generated in the substrate or coming from n+ regions are attracted at the surface of the substrate
  VGS > VTH and VDS < (VGS - VTH) → ID linearly ↗ → Linear mode (or triode mode or ohmic mode): creation of a conduction channel of e- → the transistor operates like a resistor
  VGS > VTH and VDS > (VGS - VTH) → ID independent of VDS: Saturation mode (or active mode): ID / (VGS - VTH)2

## Slide 4: Saturation mode
We have VGS > VTH → when VDS ↗ → VD > VS → VG - VD < VG - VS → VGD < VGS → the density of e- decrease in the channel near the drain → the channel is pinched at point P (pinch-off point), close to the drain → ↗ of the resistance of the channel → saturation of ID
ID is thus independent (practically → weakly dependent) of VDS and principally controlled by VGS

## Slide 5: Characteristic curves ID = f(VDS)

## Slide 6: Characteristic curve ID = f(VGS)
ID
VGS
VTH

## Slide 7: Scheme of a p-type channel MOSFET (pMOS)
Similar to the n-channel MOSFET but the doped regions are opposite, ID is opposite, VGS and VDS have opposite polarities and the drain current is made of h+

## Slide 8: Effects of radiation on MOSFET (1)
The MOSFET under irradiation may be in passive mode (VGS = 0) or in active mode (VGS > 0) → VGS > 0 → the recombination ↘ → more sensitive and more linear response
Ionizing radiations produce e- - h+ pairs in the metal, the oxide coating and the semiconductor constituting the MOSFET
In the metal and in the semiconductor, the e- - h+ pairs are quickly removed because these materials have a weak resistance
On the contrary in the SiO2 (W ≈ 17 § 1 eV for SiO2) → the pairs, either immediately recombine, either split off because of the present electric field → however ≠ behaviour due to their ≠ mobility (5 to 12 orders of magnitude)
If we suppose a voltage VGS > 0
  → the e- drift to the gate and, because of their large mobility (¹ = 20 cm2 V-1s-1) → they reach the metal and leave the oxide in a time ≤ 1 ps
  → the h+ drift to the SiO2-Si interface more slowly because of their small mobility (strongly dependent on T → ¹ = 10-4-10-11 cm2 V-1s-1) and are trapped at the interface (always in the oxide) → giving origin to a fixed + charge → modification of the characteristic curve of the MOSFET

## Slide 9: Effects of radiation on MOSFET (2)

## Slide 10: h+ transport in the SiO2
Due to the small mobility of the h+ → the transport in the oxide can take a few seconds (depending on T)
Model for the transport of the h+ in the SiO2 → « Small Polaron Hopping » (SPH): transport (or hop) of the small (charge confined in a small volume) polaron (quasi-particle composed of a charge and of its polarization field)
SPH model based on the strong interaction between the h+ and the lattice → the interaction gives origin to a distortion of the lattice close to the h+→ ↘ of the energy of the system
The h+ polarizes the medium → this polarization then interacts back on the carrier → implies a large distortion of the lattice in the immediate vicinity of the h+ → the h+ becomes localized at a particular site → ↗ of the effective mass of the h+
The carrier, which is in practice self-trapped, is called small polaron

## Slide 11: SPH model
Initially empty localized trap
Capture of a h+ by a site → distortion of the lattice potential around the trap site
Thermal fluctuations of the system → interaction with another site → transfer of the h+ by tunnel effect
Final state

## Slide 12: Trapping of the h+ at the interface SiO2-Si (1)
When the radiation-induced h+ have completed the crossing of the oxide → they are trapped at the SiO2-Si interface → production of a + charge QT at the SiO2-Si interface
Consequently → production of a - image charge at the surface of the semiconductor
  → has a positive role in the formation of the n-channel for a nMOS → the voltage to be applied to the gate to create the n-channel is smaller → VTH ↘
  → has a negative role in the formation of the p-channel for a pMOS → ↗ of the |VGS| to be applied to have the formation of the p-channel p → VTH ↘
QT implies thus a (negative) modification ¢VTH of the threshold voltage VTH (but also to a lesser extent of the leakage current) → shift of the ID - VGS characteristic curve
This modification ¢VTH can stay for a period of time varying from milliseconds to years
¢VTH is a measure of the dose absorbed in the oxide

## Slide 13: Trapping of the h+ at the interface SiO2-Si (2)

## Slide 14: Modification of the ID - VGS characteristic curve
Modification of the ID - VGS characteristic curve for a nMOS exposed to ionizing radiation
ID
VGS
VTHavant
VTHaprès
¢VTH

## Slide 15: Mathematical expression of ¢VTH
In active mode (VGS > 0) → we consider q: the e- charge, εox: the permittivity of the oxide, ½ox: the density of the oxide, W: the energy necessary to create one e- - h+ pair, fy(E): the fraction of created charges which do not recombine, ft(E): the fraction of trapped holes, dox: the thickness of the oxide coating, D: the dose →
In passive mode (VGS = 0) → decrease of sensitivity and loss of linearity →